## Slide 1: Observation of sub-Bragg diffraction of waves
Simon R. Huisman, Rajesh V. Nair, Alex Hartsuiker,
Léon A. Woldering, Allard P. Mosk, Willem L. Vos
s.r.huisman@utwente.nl

## Slide 2: Waves in periodic media
The propagation and scattering of waves are strongly modified by periodic structures.
Stopgaps emerge due to Bragg diffraction.
Graphene
Photonic crystal waveguide
X-ray diffraction

## Slide 3: Bragg diffraction
Bragg diffraction condition:
In reciprocal space:
(von Laue)
One would expect for directions of high-symmetry, the
lowest-frequency simple-Bragg diffraction occurs at:

## Slide 4: Bragg diffraction
Bragg diffraction condition:
In reciprocal space:
(von Laue)
One would expect for directions of high-symmetry, the
lowest-frequency simple-Bragg diffraction occurs at:
This statement is wrong.
We find a significant stopband below the first-order simple-Bragg condition.

## Slide 5: Silicon 2D photonic crystals
1 mm
1 mm
  Measure reflectivity from these crystals

## Slide 6: Silicon 2D photonic crystals
1 mm
  Measure reflectivity from these crystals

## Slide 7: GM’-direction
  Agreement with calculated stopgaps
  Simple-Bragg lowest frequency.

## Slide 8: GK’-direction
  Agreement with calculated stopgaps
  Simple-Bragg not lowest frequency

## Slide 9: Simple-Bragg diffraction
  For GM’–direction diffraction on M’-point
  M’-point: Simple Bragg diffraction

## Slide 10: Simple-Bragg diffraction
  For GK–direction diffraction on B-point
  B-point: Simple Bragg diffraction

## Slide 11: Sub-Bragg diffraction
  For GK–direction diffraction also on K-point
  K-point: multiple Bragg diffraction

## Slide 12: Implications of sub-Bragg
  Valid for any type of wave in
  2D: 2 out of 5 (triangular and centred rectangular)
  3D: 7 out of 14 (including hexagonal and BCC)
  Crystallography
  Phonon scattering
  Conduction in graphene
  Critical temperature of superconductors

## Slide 13: Summary
  It’s not only simply Bragg diffraction
  There can be diffraction peaks below simple Bragg diffraction.
  Published in 2012:
  S.R. Huisman, R.V. Nair, A. Hartsuiker, L.A. Woldering, A.P. Mosk, & W.L. Vos
  Observation of sub-Bragg diffraction of waves in crystals
  Phys. Rev. Lett. 108, 083901: 1-5 (2012)
  With journal front page, available from COPS website

## Slide 14
Visit us @ CLEO:
CK6.4 MON: Ultrafast switching mechanisms of microcavities
CK7.1 MON: Coherent optical imaging through opaque layers
CK7.5 MON: Focusing light through turbid media by binary amplitude modulation
EI1.3 TUE: Ultrafast switching of photonic microcavities
EI2.4 TUE: A nanophotonic probe for quantum electrodynamics in random cavities
CI2.6 TUE: Q-factor dependent Kerr-switching of microcavities